GJFJH（3.0）-1FO

# 1. Cable cross-section

Jacket

Ar-amid yarn

Tight buffer

Optical fiber

# 2. Cable Specification

2.1 Introduction

Simplex cable use single tight buffer fiber as optical communication medium, buffer fiber wrapped with a layer of aramid yarns as strength member and cable is completed with LSZH jacket.

2.2 Fiber color code

| NO. | 1 |
| --- | --- |
| Fiber color | Natural |

2.3 Tight buffer color code

| NO. | 1 |
| --- | --- |
| Tight buffer color | Natural |

2.4 Optical fiber type and properties

G657A2 Characteristic of Optical Fiber

| Category | Description |  | Specifications |
| --- | --- | --- | --- |
|  |  |  | G.657A2 |
| Optical Specifications | Attenuation | @1310nm | ≤0.35dB/km |
|  |  | @1383nm | ≤0.35dB/km |
|  |  | @1460nm | ≤0.25dB/km |
|  |  | @1550nm | ≤0.21dB/km |
|  |  | @1625nm | ≤0.23dB/km |
|  | Attenuation vs. Wavelength | @1285~1330nm relative to@1310 | ≤0.08 dB/km |
|  |  | @1525~1575nm relative to@1550 | ≤0.05 dB/km |
|  | Zero Dispersion Wavelength |  | 1300~1324nm |
|  | Zero Dispersion Slope |  | ≤0.092ps/(nm2.km) |
|  | Dispersion | @1310nm | ≤3.5 ps/nm.km |
|  |  | @1550nm | ≤18.0 ps/nm.km |
|  |  | @1625nm | ≤22.0 ps/nm.km |
|  | Cable Cutoff Wavelength(λcc) |  | ≤1260nm |
|  | Macro-bend induced attention 10 turns around a mandrel of 15mm radius at 1550n |  | ≤0.21dB |
| Geometric Specifications | Mode Field Diameter | @1310nm | 8.6±0.4μm |
|  | Cladding Diameter |  | 125±1μm |
|  | Cladding Non-Circularity |  | ≤1.0% |
|  | Coating Diameter |  | 243±7μm |
|  | Coating/Cladding Concentricity Error |  | ≤8μm |
|  | Core/Cladding Concentricity Error |  | ≤0.5μm |
| Mechanical Specifications | Proof Test level |  | ≥1.0% |
|  | Fiber Curl Radius |  | ≥4.0m |
|  | Peak Coating Strip Force |  | 1.3~8.9N |

2.5 Cable structure and parameter

| Item |  | Parameters |
| --- | --- | --- |
| Fiber cores | Count | 1 |
| Buffer fiber | Diameter | 0.9±0.05 mm |
|  | Material | LSZH |
| Strength member | Material | Aramid yarns |
| Outer jacket | Diameter | 3.0±0. 1 mm |
|  | Material | LSZH |
|  | Color | Black |
| Tension | Short term | 700 N |
| Crush | Short term | 1000 N/100mm |
| Weather condition | / | No ice and max wind 20m/s |
| Max. span | m | 100 |
| Installation sag | % | ≥1.0 |
| Cable attenuation |  | ≤ 0.4 dB/km at 1310nm, ≤ 0.3 dB/km at 1550nm |
| Cable weight (Approx.) |  | 10 kg/km |

# 3. Characteristic of Optical Cable

3.1 Min. bending radius

Static:    10 x cable diameter

Dynamic:   20 x cable diameter

3.2 Application temperature range

Operation:   - 20C ~ +65C

Installation:   - 10C ~ +50C

Storage/transportation:   - 20C ~ +65C

3.3 Main mechanical & environmental performance test

| Item | Test Method | Acceptance Condition |
| --- | --- | --- |
| Tensile Strength IEC 60794- 1-2-E1 | - Load: Short term tension - Length of cable: ≥ 50m - Load time: 1min | - Loss change 0. 1dB@1550nm after test. - No fiber break and no sheath damage. |
| Crush Test IEC 60794- 1-2-E3 | - Load: Short term crush - Load time: 1min | - Loss change 0. 1dB@1550nm after test. - No fiber break and no sheath damage. |
| Temperature Cycling | - Temperature: -20C~+65C | - Fiber additional attenuation ≤ 0.4dB/km. |

| Item | Test Method | Acceptance Condition |
| --- | --- | --- |
| IEC 60794- 1-2-F1 | - Time of each step: 12h - Number of cycle: 2 | - No fiber break and no sheath damage. |
| Torsion IEC 60794- 1-2-E7 | - Length: 1m - Twist angle: ±90° - No. of cycle: 10 | - Loss change 0. 1dB@1550nm after test. - No fiber break and no sheath damage. |
| Water Penetration IEC 60794- 1-2-F5C | - Height of water: 1m - Sample length: 3m - Time: 1h | - No water leak from the cable core of the opposite end. |