
1. OPTICAL CABLE                                                                                                                            

1.1 Construction of cable










	Cable type
	
	12

	element
	--
	6

	Central strength member
	Material
	Fiberglass Reinforce with Plastic

	Loose Tube
	Material
	Polybutelene Terephthalate (PBT)

	
	Fibers/Tube
	6

	Filling compound in loose tube
	Material
	Thixotropic jelly

	Water blocking
	Material
	Water blocking yarn and tape

	Strength Member
	Material
	Aramid yarns

	
	kg/km
	Aprox.3.5

	Outer Sheath
	Material
	Black HDPE

	
	Thickness
	Norminal: 1.9mm

	Outer Diameter
	mm
	11.1±0.4

	Cable Weight
	kg/km
	96

	Short term tensile
	KN
	3.5


2.  TEST REQUIREMENTS  
	No
	Item
	Test standard
	Method
	Acceptance criteria

	1
	Tensile
 test
	IEC-60794-1-E1
	-Max. Tensile strength

-Sample length:50 meters

-Time: 10minutes;
	-Fiber strain at maximum 
Load: max. 0.33%

-Attenuation increase≤0.10dB

	2
	Crush
 test
	IEC-60794-1-E3
	-Load:1000N

-Time: 5minutes
-Length: 100mm

- Position: One point and one time
	-No splits or cracks in the 
outer jacket;

-Attenuation increase<0.10dB

	3
	Impact
 test
	IEC-60794-1-E4
	-Impact energy: 450g
- Height:1 meter
-Impact points: 1
--Number of impacts: 5
	-No splits or cracks in the outer jacket
-Attenuation increase≤0.10dB(after the test)

	4
	Torsion 
test
	IEC-60794-1-E7
	-1m cable length with 150N weight
-±180°, 10 cycles
	- No splits or cracks in the outer jacket

-Attenuation increase ≤0.10dB(after the test)

	5
	Repeated bending 
	IEC-60794-1-E6
	-Radius=25×cable outer diameter
-1m cable length with 150N weight,25 cycles
	- No splits or cracks in the outer jacket

-Attenuation increase ≤0.10dB(after the test)

	6
	Temperature cycling test
	IEC-60794-1-F1
	-Temperature step: +20℃→-40℃→+60℃→-40℃→+60℃→+20℃
-Time per each step: 12 hrs

-Number of cycles: 2 cycles
	-Attenuation variation for reference value(the attenuation to be measured before test at +20±3℃) ≤0.10dB/km,

	7
	Cable bending test


	IEC 60794-1-E11B
	-Diameter of mandrel :

25×diameter of cable

- Number of cycles:1 cycle
	Change of attenuation shall not be greater than 0.1dB.

No fiber break and no cable damage.

	8
	Water penetration test
	IEC-60794-1-F5
	-Water height: 1m
-Sample length:3m
-Duration of test: 24hrs
	-No water leakage at the end of the sample

	9
	Drip test
	IEC-60794-1-E14
	-Five 0.3m samples suspended vertically in a climate chamber, raised temperature to +70℃
	-No filling compound shall drip from tubes after 24 hr


Optical fiber


Loose tube


Thixotropic Jelly


Central strength member (FRP)


Water blocking tape


Water blocking yarns


Ripcord（red）


Aramid  yarns


Outer sheath (Black HDPE)









