1. OPTICAL CABLE

1.1 Construction of cable

Optical fiber

Loose tube

Thixotropic Jelly

Central strength member (FRP)

Water blocking tape

Inner sheath

Water blocking yarns

Aramid yarns

Outer sheath

Ripcords

| Item | Contents | 24 |
| --- | --- | --- |
| Span | M | 400 |
| Structure | Type | 1+6 |
| Loose tube | Fiber counts/tube | 6 |
|  | Outer diameter (mm) | 2.0±0.1 |
| Central strength member | Material | FRP |
|  | Diameter (mm) | 2.3±0.1 |
| Water blocking | Material | Water Blocking Yarn& Water Blocking Tape |
| Inner Sheath | Material | MDPE |
|  | Thickness (mm) | 0.8±0.1 |
| Strength member | Material | Armid yarn |
| Sheath | Material | HDPE |
|  | Thickness (mm) | 1.6±0.2 |
| Ripcord | Material | Polyester yarn |
|  | No. | 4 |
| Cable diameter(mm) |  | 12.5±0.5 |
| Cable weight(kg/km) Approx. |  | 110±10 |
| The wind speed(m/s) |  | 20 |
| Icing(mm) |  | 0 |
| Sag(%) |  | 1.5 |
| MAT(N) |  | 7200 |

2.TEST REQUIREMENTS

| No | Item | Test standard | Method | Acceptance criteria |
| --- | --- | --- | --- | --- |
| 1 | Tensile test | IEC-60794-1-E1 | -Max. Tensile strength -Sample length:50 meters -Time: 1minutes; | -Attenuation increase≤0.10dB |
| 2 | Crush test | IEC-60794-1-E3 | -Load:2200N -Time: 1 minutes -Length: 100mm | -No splits or cracks in the outer jacket; -Attenuation increase<0.10dB |
| 3 | Impact test | IEC-60794-1-E4 | -Impact energy: 450g - Height:1 meter -Impact points: min.1 --Number of impacts: 5 | -No splits or cracks in the outer jacket -Attenuation increase≤0.10dB(after the test) |
| 4 | Torsion test | IEC-60794-1-E7 | -1m cable length with 150N weight -±180°, 10 cycles | - No splits or cracks in the outer jacket -Attenuation increase ≤0.10dB(after the test) |
| 5 | Repeated bending | IEC-60794-1-E6 | -Radius=20×cable outer diameter -1m cable length with 150N weight,25 cycles | - No splits or cracks in the outer jacket -Attenuation increase ≤0.10dB(after the test) |
| 6 | Temperature cycling test | IEC-60794-1-F1 | - Variation of temperature: -40℃→+60℃ -Soak time: 12hrs -Number of cycles: 2 cycles | -Attenuation variation for reference value(the attenuation to be measured before test at +20±3℃) ≤0.10dB/km, |
| 7 | Cable bending test | IEC 60794-1-E11B | -Diameter of mandrel : 20×diameter of cable - Number of cycles:1 cycle | Change of attenuation shall not be greater than 0.1dB. No fiber break and no cable damage. |
| 8 | Water penetration test | IEC-60794-1-F5 | -Water height: 1m -Sample length:3m -Duration of test: 24hrs | -No water leakage at the end of the sample |
| 9 | Drip test | IEC-60794-1-E14 | -Five 0.3m samples suspended vertically in a climate chamber, raised temperature to +70℃ | -No filling compound shall drip from tubes after 24 hr |

3. PACKING AND DRUM

3.1 The cable is wound on a non-returnable wooden drum. Both ends of cable are securely fastened to drum and sealed with a shrinkable cap to prevent ingress of moisture. The following information shall be marked on the outer sheath of the cable at an interval of about 1 meter.

- Cable type and number of optical fiber

- Manufacturer name

- Month and Year of Manufacture

- Cable length

The sequential number of the cable length shall be marked on the outer sheath of the cable at an interval of 1meter ± 1%.

5.2 Drum marking, Each side of every wooden drum shall be permanently marked in a minimum of 2.5~3 cm high lettering with following:

-  Manufacture name and logo

-  Cable length

-  Cable type and number of fibers

-  Roll way

-  Gross and net weight

-End of Specification-